## Slide 1
R&D for the new neutrinoless double beta decay search experiment using CdTe
Tatsuya Kikawa (Kyoto University)
Neutrinoless double beta decay (0nbb)
CdTe505050
Semiconductor | Band gap (eV) | Electron mobility (cm2/V/s) | Hole mobility (cm2/V/s) | Density (g/cm3)
Ge | 0.67 | 3800 | 1900 | 5.33
Si | 1.11 | 1400 | 500 | 2.33
CdTe | 1.47 | 1100 | 100 | 5.85
Physics motivation
If 0nbb is observed,
-Neutrino is proved to be
Majorana particle
-Absolute mass of
neutrino is proved
Search for 0nbb
Search for the energy peak by electrons from 0nbb
Very rare decay
A large quantity of double beta decay isotope
High energy resolution detector
Low background
CdTe
CdTe is semiconductor
containing double beta
decay isotopes
Energy of electrons can
be measured by CdTe
semiconductor detector
130Te, 116Cd
High isotopic composition
High Q value→ Low background around Q value
Sum energy for the 2 electrons
2nbb
0nbb
106Cd
106Cd is capable of double beta
decay of b+EC mode
-Measure e+ energy by CdTe
semiconductor detector
-Detect two 511keV g from e+ annihilation by NaI detector
→Triple coincidence (e+ + 2 g)
→ Very low background
CdTe semiconductor detector
Large band gap
→ Usable in room temperature
Low hole mobility
→Many holes are trapped in drifting
→ Low energy resolution
(especially for a large device)
→Need to improve energy resolution for 0nbb search
Cathode
Charged particle
+
+
+
－
－
－
CdTe
hole
electron
Anode
Improve energy resolution
Bias supply
Pre-amp
FADC
CdTe detector
137Cs
g (662keV)
400V
Source
Signal
Bias
Requirement
CdTe detector
NaI detector
Idea
Measure waveform from CdTe
→Estimate the effect of hole by
analyzing the waveform
→Revise the effect of hole trapping
Waveform
Setup
CdTe detector : CdTe505050 (CLEAR-PULSE)
custom-made item, ohmic type, size of device: 5×5×5(mm)
Pre-amp : 580K (CLEAR-PULSE)
charge sensitive type, time constant:60ms→ 600ms, gain:about 11
Flash ADC : V1724 (CAEN)
sampling rate: 100MHz, dynamic range: -2~2V, resolution: 14bit
Effect of electron and hole can be seen clearly.
Drift time can be estimated from the waveform.
The larger the effect of hole is, the longer the drift time becomes.
Now continuing R&D. For 0nbb search experiment using CdTe, it is necessary to improve the energy resolution to 0.5%(FWHM) for Q value with O(10cm3) CdTe device.
convert
Energy revision
Drift time
Effect of electron
(fast)
Effect of hole
(slow)
Large effect of hole
(Ionization near anode)
Long drift time
Short drift time
Large effect of electron
(Ionization near cathode)
Time (ms)
Time (ms)
Time (ms)
FADC counts
FADC counts
FADC counts
The longer the drift time is, the lower pulse height
becomes.
→Revise the pulse height by drift time
After revision, peak for photoelectric effect can be seen.
Improved energy resolution is 2.0%(FWHM) for 662keV g ray.
Drift time (ms)
Drift time (ms)
Energy (keV)
Energy (keV)
Pulse height (FADC counts)
Pulse height (FADC counts)
# of events
# of events
Temperature dependence
Nuclide | Isotopic composition | Q value (MeV)
130Te | 34% | 2.53
116Cd | 7.5% | 2.80
128Te | 31% | 0.866
106Cd | 1.5% | 1.75
Photoelectric effect
Compton effect
Temperature (℃)
Temperature (℃)
Drift time (ms)
RMS of pedestal (FADC counts)
Noise becomes small if temperature becomes low.
Drift time becomes long if temperature becomes low.
→Hole mobility seems to become small if temperature becomes low.
Best energy resolution at 0℃~10℃